Summary of steps for the production of assemblies at AeroVac               06.03.2006

Mechanics:

- Feed-through conductors should not be bended in order to avoid damage of the ceramic.

- Copper tube should be welded perpendicular to the disc.

- Outside shape at the circumference should be in accordance with the drawing for the 305 remaining assembles (The already machined disks should be re-machined, in case that the corrections are impossible CERN will decide on new dimensions).

Packing:

- The assembly should be sealed inside a plastic bag.

- Then inserted into the carton tube together with flow-pack.

Welding:

- Copper should be fixed on a raised and spinning support for the welding.

- Similar setup for the welding of the feed-through.

- The LHC cover spacer LHCBLM__0008, the protection LCBLM__0010 and the welded spacer LHCBLM__0035 should be welded using a support to ensure perpendicular fixation to the disk

- Protection of the ceramics (with a heat-sink).

- Handling should be done using gloves.

- All components should be cleaned thoroughly only before welding.

Cleaning:

- First cleaning with A206 provided by Aerovac in ultrasonic bath (3 mn)

- ultrasonic cleaning in an alkaline detergent (pH=9.7) solution at 65˚C during 10 - 20 minutes. The detergent must be such as 17.40 SPAL from Cleaning Technology – CH- 1260 Nyon, to a concentration of 10 grams per litre of demineralised water. This product will be shipped by CERN to Aerovac

- immediate rinsing with ambient temperature demineralised water jet

- rinsing by immersion in a bath of ambient temperature demineralised water during at least 10 minutes

- drying in a hot air oven at 150˚C

- No cleaning after welding. Even if exceptional mark can be seen should still not be cleaned.

Other:

- Certificate should be send at every batch for the vacuum pressure reached.

- Mark a serial number on the outside head near to the S feed-through (proposed using a spark pen) and include this numbers in the certificate. (This will become effective from the next delivery of the remaining 305 pieces.)

- Manufacture three prototypes for approval of the new procedure. The three prototypes are sent to CERN by express mail (not the CERN proposed delivery chain).

- Sent pictures of new procedure’s setup, welding steps, storage of material, and equipment used (especially interested in the ultrasonic bath and leak test equipment, hot air ofen).

- Sent pictures of the different cleaning step.

- Delivery to be agreed (proposed in either batches of 100, 150 or 300)

- The second batch of 150 pieces (samples were available during visit) will be sent at 07/02/2006. (still produced without the approved cleaning procedure and expected to need further cleaning and check of out-gassing and feed-through insulation needed to be done at CERN).

- End Delivery at 31/03/2006.

- Note that transports are possible only Tuesdays or Fridays (if use the CERN approved).