# BLM_S outgassing considerations

Chamber dimensions

| Shell surface Ash | 39 103 mm2 |
| --- | --- |
| Shell volume Vsh | 593 103 mm3 |
| Electrode surf Ael | 7.5 103 mm2 |
| Spacer surf Asp | 2.3 103 mm2 |
| Spacer volume Vsp | 11 103 mm3 |
| Ceramics volume Vce | 77 103 mm3 |
| Total Steel Surface A =Ash+4 Asp | 485 cm2 |
| Inner Free Volume V = Vsh-4Vsp-Vce | 0.47 dm3 |
| Available for NEG Ash / Atube | 390 / 280 cm2 |

| Steel 316LN glow discharged – 4.7MeV/u Pb53+ induced outgassing (initial) | 2 104 molecules/ion |
| --- | --- |
| TiZrV (NEG 300°C) – 4.7MeV/u Pb53+ induced outgassing (initial) | 40 molecules/ion |
| TiZrV (NEG 200°C) – 4.7MeV/u Pb53+ induced outgassing (initial) | 220 molecules/ion |
| Steel 304L outgassing induced by 1.4MeV/u ions* | Pb27+ | 1900 molecules/ion |
|  | Cr7+ | 300 |
|  | C2+ | 10 |
| Thermal outgassing H2 (316LN) | 4.5 10-15 mbar l/s/cm2 |
| H2 pressure after 20y constant outgassing+ | 4.3 10-3 mbar = 2.2 1017 H2 |
|  | H2 | CO | N2 |
| NEG max sticking probability α | 3 10-2 | 0.9 | 3 10-2 |
| NEG Surface capacity [molec/cm2] |  | 8 1015 | 1.5 1015 |
| NEG electron induced desorption | 2 10-4 | 1 10-4 |  |
| NEG 194eV photon induced desorption | 3 10-6 | <2 108 |  |
| NEG 4.5keV photon induced desorption | 1.5 10-5 | <10-5 |  |
| 316LN electron induced desorption** | 2 10-2 | 1 10-2 |  |
| 316LN 4.5keV photon induced desorption** | 1.5 10-3 | 1 10-3 |  |

* The desorption rate scales very well with (dE/dx)2 of the incident particles!

** The steel desorption is calculated assuming 100 times higher rate than for the activated NEG coating

+ Outgassing of electrodes or ceramics not included

Molecular Adsorption rate of a Getter pump

Molecular adsorption (PUMPING) speed of a getter coating for the two dominant elements assuming the tube surface is covered by NEG at 300K and 10-6 Torr

|  | H2 | CO |
| --- | --- | --- |
| M | 2 | 28 |
| α | 3 10-2 | 0.9 |
| dθ/dt [molec/cm2/s] | 43 1012 | 345 1012 |
| dθ/dt [molec/s] | 12 1015 | 97 1015 |
| dθ/dt [Torr*l/cm2/s] | 1.3 10-6 | 11 10-6 |
| dθ/dt [Torr*l/s] | 0.38 10-3 | 3 10-3 |

| Beam lifetime | 10h | 20s |
| --- | --- | --- |
| Nominal beam intensity | 3.2 1014p+ | 3.2 1014p+ |
| Mean loss rate in collimators | 9 109 p+/s | 1.6 1013 p+/s |
| Max MIP flux seen in BLMS @ TCS1 | 4.2 109 MIP/s/cm2 | 7.4 1012 MIP/s/cm2 |
| Max MIP rate seen by STEEL surface of BLMS @ TCS1 | 2 1012 MIP/s | 3.6 1015 MIP/s |
| Max desorption rate of STEEL surface of BLMS @ TCS1 | 4 1010 H2 /s | 7.2 1013 H2 /s |
| Total dose after 20y* | 6.3 1019 MIP |  |
| Desorption from STEEL 20y | 1.2 1018 H2 |  |
| Desorption from STEEL 20y | 8 10-2 Torr (0.11mbar) |  |
| Max MIP rate seen by NEG surface of BLMS @ TCS1 | 1.2 1012 MIP/s | 2.1 1015 MIP/s |
| Total dose after 20y | 3.8 1019 MIP |  |
| Desorption from NEG 20y… | 7.6 1015 H2 |  |
| NEG CO capacity | 2.2 1018 |  |
| NEG H2 capacity ? | 2.2 1019? |  |

* According to measurements, the desorption yield (15cm2 of Cu) is constant up to 1016 and after the dose of 1019 electrons it decreases 30 times, due to surface cleaning.

Metallic Ti is normally covered by a very thin protective layer of TiO2.