|  | LHC Project Report XX |
| --- | --- |
| Simulation of beam losses with the MQM magnet. |
| Authors D. Bocian1,2, J. Halik1,2, A. Siemko1 |
| Abstract |
| This paper present the results of beam losses study in the MQM insertion quadrupole in context of quench limit. This type of magnet is the specific one since operate both in superfluid helium at 1.9 K temperature and in liquid helium at 4.5 K. The heat transport for both temperatures is different. Therefore MQM type magnets are being identified as critical ones from among all magnets with liquid helium. The subject is evaluated with a detailed approach of the thermodynamics of the superconducting cables in response to a steady-state heat load associated to beam losses. A network model of the MQM magnet is proposed to simulate heat transport and calculate of the heat source current limit. The results of the simulations show quench limits for different regimes of MQM magnet work. |
| Department or Authors' affiliation 1) AT-MTM-TF, 2)IFJ PAN Krakow |
| Presented at |

Terms and Definitions

| Term | Definition |
| --- | --- |
| CDD | CERN Drawing Directory |
| EDMS | Engineering Data Management System |
| B | Magnetic field |
| h | Heat transfer coefficient |
| Ic | Critical current |
| κ | Thermal conductivity |
| κNbTi | NbTi thermal conductivity |
| κpoly | Polyimide thermal conductivity |
| κG10 | Epoxy glass thermal conductivity |
| κSS | Stainless steel thermal conductivity |
| κHeI | He I thermal conductivity |
| Quench | A transition of the superconductor from the superconducting to the normal state. Such a transition invariably occurs if one of the three parameters: temperature, magnetic field or current density, exceeds a critical value. |
| RRR | Residual Resistance Ratio |
| ΔT | Temperature margin |
| THe | Liquid helium temperature (4.3 K at atmospheric pressure) |
| THeII | Superfluid helium temperature |
| Tb | Bath temperature |
| Tc | Critical temperature |

# Introduction

The high beam intensities in the LHC [1] require a careful control of the beam losses around the LHC ring. The beam losses, involving significant numbers of particles, may have severe consequences for 
the accelerator equipment [2]. Several systems are designed to ensure safe operation of the LHC, such as beam dumps, collimators and beam absorbers, beam instruments and magnets protection [3]. The time constant for particle losses ranges from a few (s to several seconds depending on the specific failure [4]. Protection from multiturns beam failures relies mainly on fast monitors that detect beam losses early enough to issue a beam dump request immediately if the losses exceed the acceptable level.

This note presents the results of a study of beam losses simulation in the MQM insertion quadrupole magnet [5] which has to be found as a critical one. MQM magnet is designed as twin-aperture structure and use NbTi superconducting cables for its coil. MQM operate in superfluid helium at 1.9 K temperature

and in liquid helium at 4.5 K. Cable 4 is used in all MQM type quadrupole. MQM magnets are installed, for example, in the long straight section (Q5, Q6 and Q7) [6].

In the note a network model [7] of the MQM magnet is showed. For the creation and development of the network model we are taking advantage of a well-known method, when an electrical circuit is used to model the thermal quantities [8]. Next we are using a PSPICE program to simulate electrical circuit and obtain the results. The experimental setup is presented in the note as well.  To simulate beam losses a stainless steel tape installed in the cold bore and is used as a heat source. In the note only steady-state condition is considered. The results of the simulation are useful for a quench limit calculation for the MQM magnet. The model can be used for the quench limit calculation of MB, MQ and MQY magnets, as well.

## Heat transfer

In either steady-state or transient condition, the first principle of energy conservation law must be satisfied at any instance,

Eq. 1

where Ein is the thermal input energy, Eout is the thermal output energy, Egen is the thermal generated energy. The rate of change of energy stored within the control volume is designated as dEheat/dt. Since the magnet layers (insulation, cables, helium channels), to which a heat sink, are assumed to be the sole heat dissipation path to the heat reservoir, heat conduction downwards and aside is considered in this thermal modelling. Heat convection is ignored by the application of adiabatic boundary condition. This is a reasonable assumption because, in general, the magnet is enclosed by thermally insulated package materials. Heat radiation is simply too small to be taken into account. Therefore, the heat transfer process can be quantified by the rate equation known as Fourier’s law:

Eq. 2

Where q( [W/m2] is the heat flux and κ [W/m·K] is the thermal conductivity.

## Hadronic cascades

The energy of proton

# Electrical equivalent model for thermal properties

The power dissipation in magnet components will lead to a complex process of combined heat conduction, convection and radiation. In case of superconducting magnets the dominating process is the heat conduction. In many cases a simple model for heat transfer is sufficient. It is used a well-known method, where an electrical circuit is used to model the thermal quantities. The analogy between electrical and thermal circuits is shown in the Table 1.

Table 1 The analogy of the equivalent thermal circuit

| Thermal circuit | Electrical Circuit |
| --- | --- |
| ( | [K] | Temperature | V | [V] | Voltage |
| Q | [J] | Heat | Q | [C] | Charge |
| Q | [W] | Heat transfer rate | I | [A] | Current |
| Κ | [W/Km] | Thermal Conductivity | Σ | [1/Ωm] | Electrical Conductivity |
| RΘ | [K/W] | Thermal Resistance | R | [V/A] | Resistance |
| CΘ | [J/K] | Thermal Capacitance | C | [C/V] | Capacitance |

The analogy between electrical and thermal circuit can be expressed in following:

- steady-state condition

Temperature rise     (      Voltage difference

- transient condition

Heat diffusion               (     RC transmission line

Figure 1 shows an example of the electrical circuit, which represents thermal circuit, with a thermal resistance and capacitance. In figure 1 current source iΘ describes the power dissipation in the heater (quench heater) and node viltages uΘ represent the differences between the actual and the ambient temperature.

In the model, it is used an electrical equivalent circuit for describing the thermal behaviour of the components. In the simulation we are used for the simulation of the steady state only resistance, capacitance does not play a role.

## Thermal resistance and capacitance

Eq. 3

Eq. 4

where  ΔV=w· d· l is a volume, ρ – is the material density, Cp is the specific heat.

Generally thermal resistance is expressed in [K/W].

## Thermal resistance calculation for the MQM magnet

In 2-dim model heat source and resistance are normalized to 1 m in the 3rd dimension, so the heat source is in  and thermal resistance is in

For 2-dim model thermal resistance of solid elements and He I is calculated as follow:

Eq. 5

where l – is the length and w – is the width of the sample and R( is expressed in units [m(K/W].

The He II thermal resistance is calculated as follow [9]:

Eq. 6

Eq. 7

Eq. 8

where  is expressed in  units  and q is expressed in Watts.

# Network Model

## Superconducting cables

A photo and schematic cut view of the superconducting cable cross section is presented in Fig. 1. The wires are made of NbTi filaments inserted inside a Copper matrix. The Helium occupies the space between 
the wires and between the wires and insulation. A detailed characteristic of the cable and insulation 
is presented in [7].

Fig. 2 Superconducting cable photo and schematic cut view

The thermal contact between two cables is poor due to the insulation which is a barrier to the heat transport. Heat transport out of the cable is dominated by the flow of helium through the insulation. Fig.3 shows model of the cable with insulation. The μ-channel, which is occupied by the liquid helium is indicated in the figure. The μ-channel plays important role in the heat extraction for the magnets which operate in superfluid helium at 1.9 K temperature. For the magnets which operate in liquid helium 
at 4.5 K the heat conduction is comparable with the insulation, so the μ-channels are less efficient.

Fig. 3 Insulated cable. Arrow indicates a μ-channel by which heat could be extracted from the outer layer of the superconducting cables.

Table 2 shows a basic information about cable type-4 whereas table 3 summarizes information about polyimide insulation used in the cable type-4.

Table 2 Cable characteristic

| Cable type | Strand type | #strands | A-cable (mm2) | Cu (mm2) | NbTi (mm2) | He (mm2) | Insulation (mm2) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Type-4 | 5 | 36 | 6.646 | 4.229 | 2.417 | 0.429 | 1.885 |

Table 3 The insulation of cable type-4. Layer 1 and layer 2 overlaps by 50%, layer 3 is a strip layer with 
a 2 mm space occupied by liquid helium.

| Insulation | Units | Cable Type-4 |
| --- | --- | --- |
| layer 1 | mm | 0.025 |
| layer 2 | mm | 0.025 |
| layer 3 | mm | 0.056 |

In fig. 4 a detailed network model of the superconducting cable is showed. The cable have been artificially shared in thermal resistance element to show the heat flow inside the cable. Table 4 summarizes the values and input parameter for calculation of the resistance for each of resistor in the network model

Fig. 4 Superconducting cable model (left) and equivalent electrical circuit (network model). Each element of the cable model is described in table 4.

Table 4 Values used in calculation of thermal resistance for cable type-4 at temperature T=4.6 K.

| Resistance element description | Thermal resistance R( [m(K/W] | Length l [m] | Width w [m] | Depth d [m] | Thermal conductance κ [W/m(K] |
| --- | --- | --- | --- | --- | --- |
| Top insulation R101 | 5.02 | 4,226·10-5 | 9,099·10-4 | 0,82 | 1,128·10-2 |
| Helium μ-channel * R102 | 25.15 | 4,226·10-5 | 9,099·10-4 | 0,18 | 1,026·10-2 |
| Insulation R201 | 121.06 | 4,226·10-5 | 3,774·10-5 | 0.82 | 1,128·10-2 |
| Helium μ-channel * R202 | 606.33 | 4,226·10-5 | 3,774·10-5 | 0,18 | 1,026·10-2 |
| Helium μ-channel * R3 | 541.48 | 4,226·10-5 | 4,226·10-5 | 0,18 | 1,026·10-2 |
| Top insulation R4 | 7.79 | 8,0·10-5 | 9,099·10-4 | 1 | 1,128·10-2 |
| Top insulation R5 | 187.92 | 8,0·10-5 | 3,774·10-5 | 1 | 1,128·10-2 |
| Helium μ-channel * R6 | 1025.04 | 8,0·10-5 | 4,226·10-5 | 0,18 | 1,026·10-2 |
| Helium ΣR7 | 21319.91 | 8,8·10-3 | 4,023·10-5 | 1 | 1,026·10-2 |
| Metal ΣR8 | 0.05 | 8,8·10-3 | 8,4·10-4 | 1 | 220,518 |
| Aside insulation - total ** ΣR9 | 10776.45 | 8,8·10-3 | 8,0·10-5 | ** | 1,128·10-2 |
| Helium μ-channel * ΣR10 | 112754.35 | 8,8·10-3 | 4,226·10-5 | 0,18 | 1,026·10-2 |
| Bottom insulation R11 | 9.21 | 8,0·10-5 | 7,701·10-4 | 1 | 1,128·10-2 |
| Bottom insulation R1201 | 5.93 | 4,226·10-5 | 7,701·10-4 | 0.82 | 1,128·10-2 |
| Helium μ-channel * R1202 | 29.71 | 4,226·10-5 | 7,701·10-4 | 0,18 | 1,026·10-2 |
| Interconnection resistanceR78 | 4.33·10-4 | 8,4·10-4 | 8,8·10-3 | 1 | 220,518 |
| Interconnection resistanceR89 | 0.24 | ** | 8,8·10-3 | 1 | 1,128·10-2 |
| Interconnection resistance R910 | 0.45 | 4,226·10-5 | 8,8·10-3 | 1 | 1,026·10-2 |

*      - helium μ-channel efficiency is 18% i.e. 18% space is occupied by helium, rest by insulation (see fig. 3).
** - aside cable insulation consists of 2 layers of 100% insulation and 1 layer strip insulation shared with helium μ-channel (82%)

## MQM superconducting magnet

Fig. 5 View of the MQM magnet. (CORRECT THIS PICTURE)

The MQM magnet is the unique one in LHC  ring which operate in superfluid helium at 1.9 K temperature and in liquid helium at 4.5 K, as well. Because of the heat evacuation for these two regimes of work is different, it needs more attention with a quench limit calculation. For the network model it is important to establish at first the heat reservoirs. The upper reservoir for both temperatures is collar which consists of stainless steel plates and helium channels. The reservoir for the other side of collar is helium channel for magnets which operate in superfluid helium at 1.9 K and cold bore for magnets which operate in liquid helium at 1.9 K. The calculation of enthalpy of stainless steel for temperature T=4.5K gives value of 55.23 mJ/cm3.

Table 5 Magnet characteristic and cable types used in the production. The last column shows the results of energy margin (EM) from the SPQR program.

| Magnet type | Cable type | Op-T (K) | I (A) | Iultimate (A) | Pick-field (T) |
| --- | --- | --- | --- | --- | --- |
| MQM | Type-4 | 1.9 | 5390 | 5820 | 6.30 |
| MQM | Type-4 | 4.5 | 4310 | 4650 | 5.04 |

Table 6 Values used in calculation of thermal resistance for   MQM magnet at temperature T=4.6 K. R00 is a sum of thermal resistance of quench heater, 4 layers of GPI and collaring shoe (see fig. 5 and fig. 6).

| Resistance element description | Thermal resistance R( [m(K/W] | Length l [m] | Width w [m] | Depth d [m] | Thermal conductance κ [W/m(K] |
| --- | --- | --- | --- | --- | --- |
| Collaring shoe R00 | 2.45 | 7.0·10-4 | 1.071·10-3 | 1 | 2.671·10-1 |
| GPI* R01 | 10.66 | 1.25·10-4 | 1.071·10-3 | 1 | 1.095·10-2 |
| Quench heater R021+ R022 | 17.06 | 2.0·10-4 | 1.071·10-3 | 1 | 1.095·10-2 |
| Interlayer insulation R031 | 1.83 | 1.25·10-4 | 9.288·10-4 | 1 | 6.478·10-2 |
| Interlayer insulation R032 | 2.12 | 1.25·10-4 | 1.071·10-3 | 1 | 6.478·10-2 |
| Interlayer insulation R04 | 19.76 | 1.6 10-4 | 1.25·10-4 | 1 | 6.478·10-2 |
| Helium R05 | 142.21 | 1.38·10-3 | 9.288·10-4 | 1 | 1.045·10-2 |
| Cold bore insulation R06 | 10.82 | 1.1·10-4 | 9.288·10-4 | 1 | 1.095·10-2 |
| Cold bore R07 | 6.05 | 1.5·10-3 | 9.288·10-4 | 1 | 2.671·10-1 |

* 4 layers of ground insulation in total, here one layer is calculated

Table 6 summarizes values of the thermal resistance which is not showed in fig. 3, i.e. all the element (excluded cable) which plays important role in the heat conduction as is showed in fig. 6.

Fig. 6 Network model of segment of MQM magnet. Left part of the figure shows electrical circuit and right shows geometrical equivalent of this circuit. In the bottom there are two grounds, depends on the working temperature of the magnet.

# Results of simulation

The temperature margin ΔT of a superconducting magnet is in general defined at nominal current (In) as the difference between the current sharing temperature of the conductor in the design peak field (B) an the bath temperature (Tb).

The temperature margin is estimated from the following formulas:

Eq. 9

where critical current given by formula:

Eq. 10

with the slope s of the Ic(4.22K, B) was deduced from two measurement of Ic at 6 and 7 T and critical temperature Tc(B) is given by inverse Lubell formula:

Eq. 11

with for NbTi: Tc0=9.2 K, and Bc20=14.5 T.

A detailed description of the algorithm for the temperature margin estimate is given in [10]

Table 7 Results of simulation of the current necessary to quench the MQM magnet

| Magnet current I [A] | Magnetic Field B [T] | Temperature margin ΔT (K) | Quench Heater current IQH [A] |
| --- | --- | --- | --- |
|  |  |  | calculated | experiment |
| 5300 |  |  |  |  |
| 5200 |  |  |  |  |
| 5100 |  |  |  |  |
| 5000 |  |  |  |  |
| 4900 |  |  |  |  |
| 4800 |  |  |  |  |
| 4700 |  |  |  |  |
| 4650* |  |  |  |  |
| 4310** | 5.04 |  |  |  |
| 4300 | 4,9 | 0,84 | 0,84 |  |
| 4000 | 4,5 | 1,15 | 0,97 |  |
| 3000 | 3,4 | 2,11 | 1,33 |  |
| 2000 | 2,3 | 2,99 | 1,59 |  |
| 1000 | 1,1 | 3,82 | 1,80 |  |
| 100 | 0,1 | 4,52 | 1,96 |  |

* - ultimate current, ** - nominal current

# Model validation

The experiments are proposed to verify the network model of the MQM magnet and simulate of the beam losses in the magnet. There are proposed two kind of experiment. The first of them is described in section 5.1.1 and propose to use existing quench heaters (see fig. 5) and for the second one a dedicated experiment is proposed as is described in section 5.1.2.

## Experimental setups

### Experimental setup with quench heater

This kind of experimental setup can be used for the temperatures of order of 4.5 K because of limitation of quench heater current due to the cables used in the quench heater connections. A detailed quench heater connection for MQM magnet is showed in the CDD drawing nr …… whereas detailed description of the cables can be found in ….. The results of the simulation for different currents of the magnet and results of few experiments are presented in table8. There are two types of experiment with quench heater:

- setting of magnet current on the chosen level and then change quench heater current by probing every 100 mA

- setting of quench heater current for the chosen magnet current below of quench limit, wait for 5 min and then ramping of magnet current with the step of 1 A/s

From the point of view of steady state the experiment type B is better due to the long time of heating of quench heater (i.e. steady state) before ramping of magnet current.

Table 8 Results of simulation of the current necessary to quench the outer layer of MQM coil at 4.54 K.

| Tested magnet name and number | Magnet current I [A] | Magnetic Field B [T] | Temperature margin ΔT (K) | Simulations | experiment R = 13.2 Ω p=1.35 bar | Current in cable [mA]≡[mW/m] | QUENCH LIMIT [mW/cm3] |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Quench Heater current IQH [A] | Delay time t [s] |  |  |
|  | 5300 | 4.28 | 0.82 |  |  |  |  |  |
|  | 5200 | 4.20 | 0.91 |  |  |  |  |  |
|  | 5100 | 4.12 | 0.89 |  |  |  |  |  |
|  | 5000 | 4.04 | 1.07 |  |  |  |  |  |
|  | 4900 | 3.96 | 1.16 |  |  |  |  |  |
|  | 4800 | 3.88 | 1.24 |  |  |  |  |  |
|  | 4717 | 3.81 | 1.31 |  | 0.0 | 0 |  |  |
|  | 4700 | 3.80 | 1.32 | 1.66 |  |  |  |  |
| SSS 627 | 4650* | 3.76 | 1.36 | 1.69 | 1.65 | 19 |  | 0.75 / 0.72 |
|  | 4600 | 3.72 | 1.40 | 1.71 |  |  |  |  |
|  | 4550 | 3.68 | 1.44 | 1.74 |  |  |  |  |
|  | 4500 | 3.63 | 1.48 | 1.76 |  |  |  |  |
| SSS 627 | 4472 | 3.61 | 1,50 | 1.77 | 1.70 | 300+50+72 |  | 0.83 / 0.76 |
| SSS 627 | 4450 | 3.59 | 1.52 | 1.79 | 1.80 | 42 |  | 0.84 / 0.86 |
|  | 4400 | 3.55 | 1.56 | 1.81 |  |  |  |  |
| SSS 627 | 4310** | 3.48 | 1.63 | 1.85 | 2.00 | 22 | 3.003 | 0.90 / 1.06 |
|  |  |  |  |  | 2.00 | 300+?+? |  |  |
|  | 4000 | 3.23 | 1.87 |  |  |  |  |  |
|  | 3000 | 2.42 | 2.62 |  |  |  |  |  |
|  | 2000 | 1.62 | 3.33 |  |  |  |  |  |
|  | 1000 | 0.81 | 4.01 |  |  |  |  |  |
|  | 100 | 0.08 | 4.60 |  |  |  |  |  |

* - ultimate current, ** - nominal current

| Imagnet [A] | Quench Limit [W/cm3] |
| --- | --- |
|  | simulations | experiment |
| 4650 | 0,75 | 0,72 |
| 4450 | 0,84 | 0,86 |
| 4310 | 0,9 | 1,06 |
| 4472 | 0,83 | 0,76 |

### A dedicated project

An experimental setup is presented in fig.6. Beam loss cascade is about 1 m long and therefore length 
of the heating source (stainless steel tape) is 1 meter long. Other dimensions are 15 mm wide and 25 μm thick according to the standard width and thickness of quench heaters. Quench heater is insulated with polyimide tapes of 75 μm thick in total and 25 μm thick of glue. It is proposed to install 8 arcs inside the cold bore, powered in series of 4 arcs.

Fig. 7 Experimental setup model

The heating elements are placed on the pipe made from material with the small heat conductance and small heat capacity.

The proposed materials, which are often used in very low temperatures, are: Stainless Steel, Copper, Aluminium or Vetronit? For our studies the best is Stainless Steel but it could be technically difficult to made this kind of construction due to the enormous high forces needed to unbend for example 
2 mm thick pipe. Vetronit has excellent mechanical, electric, chemical resistance, suitable for low temperatures.

Table 9 Thermal parameters of proposed materials at temperature T = 4.6K

| Material | CP [J/kg K] | κ (10-3 [W/m K] | ρ [kg/m3] |
| --- | --- | --- | --- |
| Aluminium | 0.31016 | 353.29 |  |
| Copper | 0.11774 | 330.35 | 8930 |
| Stainless Steel | 2.1703 | 0.27425 |  |
| Vetronit |  | 0.25 | 1900 |
| Epoxy glass G10 | 0.5573 | 0.64777 | 1790 |

## Experimental setup network model

Fig. 8 Network model of segment of MQM magnet. Top part of the figure shows electrical circuit and bottom shows geometrical equivalent of this circuit.

## Power dissipated in the magnets due to the heat source .

Eq. 12

where     P – is the power dissipated in the heater surface in [W],

R – is the resistance in [Ω],

I – is the current in [A],

S – is the heater surface in [m2],

hw – is the heater width in [m],

hL – is the heater length in [m],

w – is the cable width in [m].

For the MQM magnet at temperature T = 4.6 K:

# Conclusions

The method of the beam losses presented in the note has been never used. The results of the simulation and experiment shows …..

# Acknowledgements

The authors would like to thank  B. Auchmann, M. Calvi, G. D’Angelo, N. Catalan Lasheras, G. Beziuk,

A. Bonasia, B.Dehning, J. Kapłon, L. Oberli, R. Ostojic, P. Pugnat, S. Russenschuck, D. Tommasini for supporting this work and useful discussions.

# Bibliography

- Beam Parameters, http://lhc.web.cern.ch/lhc/,

- Schmidt R. et al., Beam loss scenarios and strategies for machine protection at the LHC,
 LHC Project Report 665, CERN, (2003),

- Jeanneret J.B., Measurement of the beam losses in the LHC rings, LHC-BLM-ES-0001.00, (2003)

- Bordry F.et al., Machine protection for the LHC: Architecture of the beam and powering interlock systems, LHC Project Report 521, (2001),

- LHC-MQM-CI-0001,

- CERN CDD drawings LHCVC1I_0001, LHCVC1I_0002, LHCVC1I_0003, http://edms.cern.ch/,

- Bocian D., Calvi M. and Siemko A., Stability Margin Calculations for the LHC Magnets, 
LHC Project Note in preparation,

- For example ……..PSPICE manual ….

- CRYOGENIE et ses applications en supraconductivite, IIF/IIR,

- Pojer M. et al, LHC Project Report 807, CERN, 2004,

- Burnod L.and Jeanneret J.B., CERN SL/91-39 (EA),

- Van Sciver S.W., Helium Cryogenic, Plenum Press, New York, 1986,

- Holman J.P., Heat transfer ; 9th ed,. New York, NY: McGraw-Hill, 2002,

- Weisend II J.G. , Handbook of Cryogenic Engineering, Taylor&Francis, 1998,

- CAS Supoerconductivity in particle accelerators, Haus Rissen, Hamburg, 1995,

Appendix A: MQM magnet characteristic

Table A.1 MQM magnet field map

| Conductor | Field [T] | Conductor | Field [B] |
| --- | --- | --- | --- |
| 1 | 3.2897 | 16 | 1.2699 |
| 2 | 3.3210 | 17 | 1.3385 |
| 3 | 3.3869 | 18 | 1.4533 |
| 4 | 3.4843 | 19 | 1.5953 |
| 5 | 3.6103 | 20 | 1.7565 |
| 6 | 3.7628 | 21 | 1.9327 |
| 7 | 3.9408 | 22 | 2.1215 |
| 8 | 4.1447 | 23 | 2.3217 |
| 9 | 4.3765 | 24 | 2.5326 |
| 10 | 4.6425 | 25 | 2.7540 |
| 11 | 4.4005 | 26 | 2.9855 |
| 12 | 4.8132 | 27 | 3.2262 |
| 13 | 5.2282 | 28 | 3.4743 |
| 14 | 5.6583 | 29 | 3.1381 |
| 15 | 6.1158 | 30 | 3.4204 |
|  |  | 31 | 3.7087 |
|  |  | 32 | 4.0198 |
|  |  | 33 | 4.3538 |
|  |  | 34 | 4.7125 |
|  |  | 35 | 5.1012 |
|  |  | 36 | 5.5308 |

Appendix B Thermal conductance of material used in the MQM magnet

Table B. 1 Thermal conductance of solid materials. For NbTi the contribution to the thermal conductance from electric conductance due to the structure defects is not significant.

| Temperature | κNbTi [W/mK] | κpoly (10-3 [W/mK] | κG10 (10-3 [W/mK] | κStainless Steal(10-3 [W/mK] | Copper (Cu) - κCu [W/mK], RRR=100 |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | MQM B=6.30 T | MQM B=5.04 T |
| 1.90 K | 12.345 | 3.4839 | 20.424 | 96.39 | 117.49 | 136.44 |
| 2.16 K | 14.031 | 4.0555 | 25.554 | 112.40 | 133.57 | 155.10 |
| 2.17 K | 14.096 | 4.0785 | 25.753 | 113.02 | 134.19 | 155.82 |
| 2.50 K | 16.234 | 4.8774 | 32.234 | 133.58 | 154.59 | 179.51 |
| 3.00 K | 19.466 | 6.2249 | 41.588 | 165.33 | 185.48 | 215.38 |
| 3.50 K | 22.688 | 7.7078 | 49.783 | 198.04 | 216.35 | 251.23 |
| 4.00 K | 25.894 | 9.2914 | 57.109 | 231.89 | 247.19 | 287.04 |
| 4.10 K | 26.533 | 9.6175 | 58.467 | 238.82 | 253.35 | 294.20 |
| 4.20 K | 27.171 | 9.9462 | 29.791 | 245.79 | 259.51 | 301.35 |
| 4.30 K | 27.808 | 10.277 | 61.083 | 252.82 | 265.67 | 308.50 |
| 4.40 K | 28.445 | 10.611 | 62.345 | 259.91 | 271.82 | 315.65 |
| 4.50 K | 29.080 | 10.946 | 63.576 | 267.05 | 277.98 | 322.79 |
| 4.60 K | 29.715 | 11.283 | 64.777 | 274.25 | 284.13 | 329.93 |
| 4.70 K | 30.348 | 11.622 | 65.952 | 281.50 | 290.27 | 337.07 |
| 4.80 K | 30.981 | 11.963 | 67.099 | 288.82 | 296.42 | 344.20 |
| 4.90 K | 31.612 | 12.305 | 68.221 | 296.19 | 302.56 | 351.33 |
| 5.00 K | 32.242 | 12.649 | 69.317 | 303.62 | 308.69 | 358.46 |
| 5.50 K | 35.373 | 14.383 | 74.461 | 341.68 | - | - |
| 6.00 K | 38.468 | 16.138 | 79.116 | 381.29 | 369.82 | 429.44 |

Table B. 2 Helium parameters

| Temperature | CP [J/kg K] | κHel (10-3 [W/mK] | ρHeI [kg/m3] | Temperature | CP [J/kg K] | κHel (10-3 [W/mK] | ρHeI [kg/m3] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 2.16 K | 11462.00 | 16.524 | 148.61 | 4.70 K | 9254.30 | 10.355 | 19.82 |
| 2.17 K | 6526.70 | 16.536 | 148.59 | 4.80 K | 8640.00 | 10.451 | 18.68 |
| 2.50 K | 2180.10 | 16.946 | 146.77 | 4.90 K | 8172.60 | 10.547 | 17.76 |
| 3.00 K | 2461.50 | 17.567 | 144.02 | 5.00 K | 7854.00 | 10.643 | 16.99 |
| 3.50 K | 3216.30 | 18.187 | 138.12 | 5.50 K | 6873.80 | 11.308 | 14.12 |
| 4.00 K | 4232.40 | 18.808 | 130.70 | 6.00 K | 6411.00 | 11.975 | 12.30 |
| 4.10 K | 4539.00 | 18.866 | 128.69 | 6.50 K | 6127.70 | 12.643 | 10.97 |
| 4.20 K | 4868.20 | 16.288 | 126.68 | 7.00 K | 5949.20 | 13.293 | 9.96 |
| 4.30 K | 5327.20 | 16.275 | 124.63 | 7.50 K | 5736.90 | 14.570 | 8.42 |
| 4.40 K | 5906.20 | 16.263 | 74.88 | 8.00 K | 5658.70 | 15.209 | 7.85 |
| 4.50 K | 10142.00 | 10.448 | 20.14 | 9.50 K | 5589.30 | 15.847 | 7.33 |
| 4.60 K | 10203.00 | 10.259 | 19.73 | 10.00 K | 5554.50 | 16.400 | 6.90 |

Fig.B-1 Helium I heat capacitance and heat conductivity distribution.

# Footnotes

In case of helium μ-channels 0.18 m is occupied by helium, rest by insulation as showed in fig. 3. An importance of helium μ-channels is discussed in section 3.1.

This pressure correspond the temperature of ~ 4.535 K

# Endnotes

- Beam Parameters, http://lhc.web.cern.ch/lhc/;

- R. Schmidt et al., Beam loss scenarios and strategies for machine protection at the LHC,
 LHC Project Report 665, CERN, (2003);

- J.B. Jeanneret, Measurement of the beam losses in the LHC rings, LHC-BLM-ES-0001.00, (2003)

- F. Bordry et al., Machine protection for the LHC: Architecture of the beam and powering interlock systems, LHC Project Report 521, (2001)

- LHC-MQM-CI-0001

- CERN CDD drawings LHCVC1I_0001, LHCVC1I_0002, LHCVC1I_0003, http://edms.cern.ch/;

- D. Bocian, M. Calvi and A. Siemko, LHC Project Note in preparation

- For example ……..

- CRYOGENIE et ses applications en supraconductivite, IIF/IIR

- M. Pojer et al, LHC Project Report 807, CERN, 2004,

Introduction – short info about

Beam losses

network model (refer to the previous note)

parameters calculations (Resistance), some theory?

Heat transfer – two elements of heat transfer

experiment descriptions + figures (CDD drawings), coil model – ROXIE, magnet model with insulation, enthalpy of heat reservoir

simulation of the experiment with the network model

Results

Network Model Note:

- Some basic info about network model

- Experiment description, CDD drawings

- Resistance calculation method

- Helium channels – μ-channel (efficiency 2/11=18%) and between cold bore and inner layer

- Cold bore and insulation

- Interlayer insulation

- Field maps for all magnets – Temp. margin ΔT calculation

- Quench heaters active surface

- Collar, yoke, etc.

- Parameters, convection, etc.

# Text boxes

l

d

Fig. 1 Network model of heat transport. Current source iΘ describes the power dissipation, RΘ is a thermal resistance and CΘ is a thermal capacitance

I

iΘ

C2Θ

C2Θ

R1Θ

R2Θ

w