# EDMS No.:  xxxxxx

# DR-02058/AB/LHC

# DO-21530/AB/LHC

# Technical Specification

# Feed-Through

# Dimensions according to the Technical drawing CDD No.: LHCBLM__0002 and LHCBLM__0003.

# The General Technical Specification, EDMS 581010, in its actual version, constitutes an integral part of this document.

Number of pieces:

Baseline:	7420

Option:	1760

# UHV current feed-throughs with the dimension according to the technical drawing LHCBLM__0002 and LHCBLM__0003 – corresponding to CERAMSEAL 3887-12-W.

# Material: 	Outside: 	stainless steel

# Current lead:	copper

# Voltage:	>3000V

# Current:	>15mA

# Leak rate:	<10E-10 mbar l/s

The feed-throughs will be used in an UHV application. They have to be delivered clean for UHV application and must not outgas. They have to withstand baking at 300 C.